## Slide 1
2022
文献阅读
2022.9.7
汇报人：20224214106-金润君
Notes: 本PPT模板部分元素使用了幻灯片母版制作。如果需要修改，点击-视图-幻灯片母版-修改；完成后关闭编辑母版即可。

## Slide 3
02
03
04
总结与结论
结果与讨论
实验
01
背景
CONTENT

## Slide 4
PART
背景
01

## Slide 5
背景
有机-无机杂化钙钛矿
太阳能电池
空穴传输层
钙钛矿层
此文献的研究对象主体
电子传输层
基底电极
太阳能电池的器件结构p-i-n
此文献是n-i-p结构，
即将空穴传输层与电子传输层交换。
电极

## Slide 6
背景
Figure 1. (a) The schematic device structure of ITO/PEDOT:PSS/Perovskite/PCBM/Ag; (b) the energy level diagram
图一的能级分布也印证了上述n-i-p结构
(a)
(b)

## Slide 7
背景
经典三维钙钛矿的结构：ABX3 (图二)
A是有机离子，如甲铵离子（CH3NH2+,MA）和甲脒离子 (H2NCHNH+, FA).
B是金属阳离子，一般为Pb2+和Sn2+.
X是卤素阴离子.
Figure 2. Schematic diagram of perovskite structure.
此文献中，将研究A位点储有机离子的混合（MA-FA）对太阳能电池性能的影响

## Slide 8
PART
02
实验

## Slide 9
实验
每次旋涂后均需退火
PEDOT:PSS
ITO
ITO
…
两步旋涂法
PbI2+(MAI and FAI)
ITO
PEDOT:PSS
FAxMA1-xPbI3
PCBE
Ag
…
旋涂
旋涂
退火
退火
旋涂
退火
旋涂
退火
此文献中还在PCBM(电子传输材料)与Ag之间加入一层Bphen

## Slide 10
PART
03
结果与讨论

## Slide 11
结果与讨论
Figure 3. (a–f) Top-view SEM images of FAxMA1-xPbI3 Perovskite films with different FA+ ratio (x = 0, 0.2, 0.4, 0.6, 0.8, and 1).
颗粒大小能够被FA含量调控，随着FA增加而增大。
FA0.4MA0.6PbI3具有致密的表面和大晶粒，与相邻层的连接提升。

## Slide 12
结果与讨论
Figure 4. (a) The XRD patterns of the FAxMA1-xPbI3 (x = 0, 0.2, 0.4, 0.6, 0.8, and 1) perovskite film; (b) Enlarged XRD area around 14°. (c) The lattice spacing of FAxMA1-xPbI3 (x = 0, 0.2, 0.4, 0.6, 0.8, and 1) film with different FA+ ratio.
FAxMA1-xPbI3是与MAPbI3具有相同晶体结构的固溶体(Figure 4a)
由于FA的掺杂，导致了晶格膨胀(Figure 4b中衍射峰向低角度方向偏移)
Figure 4c展示了晶格膨胀与FA含量的线性关系。

## Slide 13
结果与讨论
Figure 5. The UV/Vis absorption spectra of the perovskites FAxMA1-xPbI3 (x = 0, 0.2, 0.4, 0.6, 0.8, and 1) film for various FA compositions.
随着FA含量的增加，吸收边缘 向着长波方向移动。
随着FA的增加，带隙从1.579 eV不断减小到1.479 eV

## Slide 14
结果与讨论
Figure 6. (a) Current density–voltage (J-V) curves of the perovskite solar cell with FAxMA1-xPbI3 (x = 0, 0.2, 0.4, 0.6, 0.8, and 1) without Bphen layer. (b) with Bphen layer.
FAxMA1-xPbI3的功率转换效率(PCE)比纯的MAPbI3和FAPbI3都高
FA0.4MA0.6PbI3的PCE达到了9.71%, 且此组分开路电压达到最大值
另外，器件方面的Bphen(4,7-二苯基-1,10-菲罗啉, 4,7-biphenyl-1,10-phenanthroline)层也起到了优化作用(Figure 6b)
(a)
(b)

## Slide 15
结果与讨论
Figure 7. (a) The average PCE of the FAxMA1-xPbI3 (x = 0, 0.2, 0.4, 0.6, 0.8, and 1) device with and without Bphen layer. (the red line is the device with Bphen layer, the black line is the device without Bphen layer.) (b) Long-term stabilities of the best perovskite devices FA0.4MA0.6PbI3 without encapsulation under ambient air conditions for more than half month.
PCE存在极值, 极值点与SEM中最大晶粒和最好表面致密度的点对应
Bphen层起到了提升PCE(Figure 7a 红线)和长期稳定性(Figure 7b)的作用
(a)
(b)

## Slide 16
结果与讨论
Figure 8. (a) Density of states of MAPbI3, FA0.5MA0.5PbI3, and FAPbI3. (b) The simulated absorbance of the MAPbI3, FA0.5MA0.5PbI3 and FAPbI3.
第一性原理计算表明价带顶部(VBM)能级基本不变，而导带底部(CBM)能级向费米能级靠近（当FA增加时），导致了带隙随着FA含量增加而减小(Figure 8a)
FAPbI3的带隙比MAPbI3的窄，这也从另一个方面解释了为什么随着FA增加，带隙减小的现象(Figure 8b)
带隙通过FA含量的改变而实现可调

## Slide 17
PART
04
总结与结论

## Slide 18
总结与讨论
FA0.4MA0.6PbI3达到了同系列固溶体中的性能最大值(PCE = 9.7%)
电子传输层(PCBM)与电极之间可以通过Bphen (4,7-二苯基-1,10-菲罗啉, 4,7-biphenyl-1,10-phenanthroline)层修饰，从而提升整体器件的性能(PCE = 10.86%, 具有Bphen的FA0.4MA0.6PbI3太阳能电池)
Bphen层起到了保护和减少电子传输层与电极之间的电荷传输阻碍的作用
带隙通过FA含量的改变而实现可调

## Slide 19
恳请老师同学批评指正
2022
2022.9.8
汇报人：20224214106-金润君
Notes: 本PPT模板部分元素使用了幻灯片母版制作。如果需要修改，点击-视图-幻灯片母版-修改；完成后关闭编辑母版即可。